## Slide 1
SEMICONDUCTOR ENGINEERING PRESENTATION
01 / 20
EUV, 파장 너머의 문제
Pattern Transfer에서 Platform Economics까지
01
Pattern
Transfer
02
Resolution
Limit
03
DUV
Extension
04
EUV
Transition
05
Platform
Economics
KEY MESSAGE
PHOTO는 pattern을 wafer 위 target film에 전사하는 기술이다.
미세화가 진행될수록 wavelength 하나가 아니라 optics · PR · source · scanner가 함께 움직여야 한다.
EUV의 양산 가치는 resolution · defect · throughput · cost를 동시에 만족하는 platform에서 생긴다.
Reference · ASML · Rayleigh criterion; ASML · EUV lithography systems
Notes: [Sources]
- https://www.asml.com/en/technology/lithography-principles/rayleigh-criterion
- https://www.asml.com/en/products/euv-lithography-systems
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 2
PATTERN TRANSFER
02 / 20
PHOTO의 본질은 PR 형상을 target film으로 옮기는 것이다
POSITIVE PR SEQUENCE
PR → TARGET FILM
→
→
→
→
PR COATING
EXPOSURE
DEVELOP
ETCH
PR STRIP
Wafer / Substrate
Target Film
PR
Wafer / Substrate
Target Film
PR
Wafer / Substrate
Target Film
PR
PR
Wafer / Substrate
Target
Film
PR
PR
Wafer / Substrate
Target
Film
PR stripped
노광된 positive PR 영역의 용해도 ↑
PR이 없는 곳의 target film을 제거
WHAT IS THE TARGET?
NOT THE BULK WAFER
TARGET FILM EXAMPLES
Oxide · Nitride · Metal
Poly-Si · Hard mask
PHOTO + RESIST
직관적 역할 구분
PHOTO
빛에 반응해 chemical solubility가 바뀐다.
RESIST
Develop 이후 etch 등에서 후속 pattern-transfer mask가 된다.
TRANSFER RESULT
PR에 생긴 opening이 target film의 형상으로 남는다.
‘photo-sensitive material + resist material’이라는 엄밀한 화학 정의가 아니라 역할을 이해하기 위한 표현
Reference · Tokyo Electron · The principle of Semiconductor; ASML · How microchips are made
Notes: [Sources]
- https://www.tel.com/museum/exhibition/process/process2.html?page=2
- https://www.asml.com/en/technology/all-about-microchips/how-microchips-are-made
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 3
RESOLUTION LIMIT
03 / 20
RAYLEIGH CRITERION
Resolution은 λ·NA·k1이 함께 정한다
CD ≈ k₁ × λ / NA
λ wavelength NA acceptance of optical system k₁ process factor
READING THE NUMBER
NA ↑ → imaging capability ↑ → resolution limit CD ↓
DUV VS EUV
DUV: projection lens NA
EUV: projection mirror optics NA
ACCEPTANCE CONE
고각 회절광 = 고공간주파수 정보
WAFER PATTERN
High NA · wide acceptance
Low NA · narrow acceptance
0th
±1st diffraction orders
NA는 ‘빛을 더 잘 꺾는 정도’가 아니라 optical system이 받아들일 수 있는 angular range다.
Reference · ASML · The Rayleigh criterion for resolution
Notes: [Sources]
- https://www.asml.com/en/technology/lithography-principles/rayleigh-criterion
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 4
RESOLUTION LIMIT
04 / 20
OPC = LOW-K₁ ENABLER
k₁을 낮출수록 같은 장비를 한계에 가깝게 쓴다
K₁ ↓
같은 λ와 NA에서 더 작은 feature를 요구한다.
THE COST OF LOW-K₁
Image contrast · process margin ↓
Dose · focus · mask · PR variation sensitivity ↑
낮은 k₁ = 무조건 좋은 공정
이 아니라 optical limit에 가까운 공정
MASK → OPTICAL IMAGE → WAFER
보정 전 / 보정 후
→
→
LITERAL MASK
PRINTED RESULT
rounded / shortened
OPC-CORRECTED MASK
PRINTED RESULT
target에 가까운 geometry
OPC
Diffraction과 imaging error를 미리 계산해 mask geometry를 의도적으로 보정하는 computational lithography
OPC는 ‘mask를 이상하게 그리는 기술’이 아니라 low-k₁ lithography를 가능하게 한 핵심 RET다.
Reference · ASML · Pushing k1 further; ASML · Computational lithography
Notes: [Sources]
- https://www.asml.com/en/technology/lithography-principles/pushing-k1-further
- https://www.asml.com/en/products/computational-lithography
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 5
DUV EXTENSION
05 / 20
ARF = SOURCE, NOT LENS
ArF immersion은 193 nm를 유지하면서 NA를 1.35까지 높였다
OPTICAL PATH
TRANSMISSIVE RETICLE + REFRACTIVE LENS
→
→
→
→
SOURCE
ArF excimer
193 nm
ILLUMINATION
Angle · pupil
control
RETICLE
Transmissive
pattern
PROJECTION
Refractive
lens
LAST GAP
Water
↓
Wafer PR
Immersion water는 projection lens의 마지막 optical element와 wafer PR 사이에 있다.
PRODUCTION SCALE
TOOL-LEVEL
WATER-BASED ARF IMMERSION
NA 1.35
38–40 nm
production resolution
ARF
Argon Fluoride excimer laser source
λ = 193 nm
IMMERSION
Water의 refractive index를 이용해 optical-system NA를 높인다.
INTERPRETATION
38–40 nm는 node name이 아니라 tool-level single-patterning resolution이다.
Reference · ASML · Lenses & mirrors; ASML · Light & lasers; TWINSCAN NXT:2000i / 2050i
Notes: [Sources]
- https://www.asml.com/technology/lithography-principles/lenses-and-mirrors
- https://www.asml.com/en/technology/lithography-principles/light-and-lasers
- https://www.asml.com/en/products/duv-lithography-systems/twinscan-nxt2000i
- https://www.asml.com/en/en/products/duv-lithography-systems/twinscan-nxt2050i
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 6
RESOLUTION LIMIT
06 / 20
Λ ALONE DOES NOT SET RESOLUTION
193 ÷ 13.5 ≈ 14.3, 그러나 실제 resolution은 14배가 아니다
CD ≈ k₁ × λ / NA
Wavelength advantage is filtered through NA and k₁.
ARF IMMERSION DUV
193 nm
NA ≈ 1.35
38–40 nm
PRODUCTION RESOLUTION
LOW-NA EUV · NXE
13.5 nm
NA = 0.33
≈ 13 nm
PRODUCTION RESOLUTION
HIGH-NA EUV · EXE
13.5 nm
NA = 0.55
≈ 8 nm
PRODUCTION RESOLUTION
같은 13.5 nm에서도 NA 0.33 → 0.55가 imaging capability를 바꾼다.
비교 수치는 각 ASML platform의 공식 production-resolution 표기이며 공정 node 명칭과 동일하지 않다.
Reference · ASML · NXT:2050i; NXE:3400C; EXE:5200B
Notes: [Sources]
- https://www.asml.com/en/en/products/duv-lithography-systems/twinscan-nxt2050i
- https://www.asml.com/en/products/euv-lithography-systems/twinscan-nxe3400c
- https://www.asml.com/products/euv-lithography-systems/twinscan-exe-5200b
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 7
DUV EXTENSION
07 / 20
LELE ≠ SELF-ALIGNED SPACER PATTERNING
Multi-patterning은 density를 늘리지만 공정·overlay·비용도 늘린다
LELE
MULTIPLE LITHOGRAPHY
LITHO → ETCH → LITHO → ETCH
두 번의 independent exposure를 분해해 pitch를 줄인다.
Overlay 관리가 핵심 부담이다.
Mask A
Mask B
Independent exposure 간 overlay opportunity
SADP → SAQP
SELF-ALIGNED SPACER SEQUENCE
→
→
→
→
MANDREL
CONFORMAL SPACER
ANISOTROPIC ETCH
MANDREL REMOVAL
PATTERN TRANSFER
target
target
target
target
target
sacrificial core
sidewall only
density ≈ 2×
SAQP
Spacer-derived structure를 다시 mandrel처럼 사용해 spacer patterning을 한 번 더 수행 → density를 다시 증가
‘공짜 resolution’이 아니다
Deposition · etch · mandrel removal · cut/block mask · metrology가 추가되어 cycle time, overlay management, process complexity, cost가 증가한다.
Reference · SPIE · Self-aligned double patterning; imec · SAQP / EUV N5 BEOL integration
Notes: [Sources]
- https://doi.org/10.1117/12.772905
- https://www.imec-int.com/en/imec-magazine/imec-magazine-march-2017/first-euv-lithography-high-volume-manufacturing-solution-for-n5-beol
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 8
EUV TRANSITION
08 / 20
PHOTON ENERGY CHANGES THE OPTICAL PLATFORM
13.5 nm는 기존 DUV lens에 그대로 넣을 수 없다
PHOTON ENERGY
E = hc / λ
13.5 nm → ≈ 92 eV
high-energy EUV photon
QUESTION
기존 DUV OPTICS 재사용?
13.5 nm 빛을 만들었다면
기존 transmissive lens에 넣으면 되는가?
NO
EUV 영역에서는 공기와 대부분의 optical material이 빛을 강하게 흡수한다.
WHAT CHANGES?
VACUUM + REFLECTIVE OPTICS
→
→
→
AIR
Strong absorption
→ high vacuum
TRANSMISSION
Lens / transmissive mask
→ unusable
REFLECTION
Mo/Si multilayer
mirror + mask
SYSTEM
Entire optical path
redesigned
흡수는 energy 소멸이 아니라 electron excitation · ionization · secondary electron · heat · chemical reaction으로의 전환이다.
Reference · ASML · Lenses & mirrors; EUV resist review · 92 eV photon / secondary electrons
Notes: [Sources]
- https://www.asml.com/technology/lithography-principles/lenses-and-mirrors
- https://pmc.ncbi.nlm.nih.gov/articles/PMC9049984/
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 9
EUV TRANSITION
09 / 20
SYSTEM ARCHITECTURE
EUV는 source부터 wafer까지 전 구간이 reflective optics in vacuum이다
Sn plasma → Collector → Intermediate Focus → Illumination → Reflective mask → Projection → Wafer PR
→
→
→
→
→
→
SOURCE
Sn plasma
EUV emission
COLLECTOR
Wide-angle
collection
IF
Intermediate
Focus
ILLUMINATION
Angle · intensity
pupil
MASK
Reflective
pattern
PROJECTION
Mirror train
demagnification
WAFER
PR records
projected image
ROLES ARE NOT INTERCHANGEABLE
각 요소의 역할 분리
COLLECTOR MIRROR
Sn plasma가 여러 방향으로 내는 EUV를 모아 optical system으로 넘긴다.
ILLUMINATION OPTICS
Reticle에 들어가는 angle · intensity · pupil condition을 형성한다.
REFLECTIVE MASK
Mo/Si reflector 위 absorber pattern으로 반사광에 pattern 정보를 싣는다.
PROJECTION OPTICS
Mask 이후 mirror system이 pattern image를 wafer PR에 축소 투영한다.
Reflective mask ≠ projection mirror · Collector ≠ illumination optics
Reference · ASML · EUV lithography systems; ASML · Lenses & mirrors; imec · High-NA EUVL
Notes: [Sources]
- https://www.asml.com/en/products/euv-lithography-systems
- https://www.asml.com/technology/lithography-principles/lenses-and-mirrors
- https://www.imec-int.com/en/articles/high-na-euvl-next-major-step-lithography
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 10
EUV REFLECTIVE OPTICS
10 / 20
COATING ≠ MAGNIFICATION
Mo/Si는 반사 coating이고, mirror geometry가 image를 만든다
MO/SI MULTILAYER COATING
13.5 NM REFLECTIVITY
Mo
Si
Mo
Si
Mo
Si
Mo
Si
Mo
Si
Mo
Si
1 period
d = tMo + tSi ≈ 6.9 nm
6.9 nm는 Mo 한 층이 아니라 Mo+Si pair의 반복 두께
MIRROR FIGURE & OPTICAL GEOMETRY
FOCUS · ABERRATION · MAGNIFICATION
CURVATURE
Focusing
POSITION
Aberration correction
ARRANGEMENT
Demagnification
Coating lets EUV survive each reflection.
Geometry determines where the image goes.
Optical coating period는 wafer circuit pitch와 아무 관련이 없다.
Reference · Montcalm et al., SPIE 3331 (1998), DOI 10.1117/12.309600; imec · EUV mask stack
Notes: [Sources]
- https://doi.org/10.1117/12.309600
- https://www.osti.gov/servlets/purl/310916
- https://www.imec-int.com/en/articles/high-na-euvl-next-major-step-lithography
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 11
EUV REFLECTIVE OPTICS
11 / 20
BRAGG-LIKE CONSTRUCTIVE INTERFERENCE
Mo/Si interface의 약한 반사가 같은 phase로 겹쳐 강해진다
GEOMETRY
Θ = GLANCING ANGLE TO MULTILAYER PLANE
wave A
wave B
d sinθ
+ d sinθ
θ
Path difference = 2d sinθ
CONDITION
SAME PHASE
mλ = 2d sinθ
θ: beam ↔ multilayer plane
ANGLE CONVENTION
Surface-normal angle α를 쓰면
mλ = 2d cosα
NEAR-NORMAL INTUITION
d ≈ λ / 2
13.5 / 2 ≈ 6.75 nm
실제 ≈ 6.9 nm는 optical constants · absorption · phase shift · interface structure를 반영한 optimized period
Reference · Underwood & Barbee, Applied Optics 20 (1981), DOI 10.1364/AO.20.003027; Montcalm et al. (1998)
Notes: [Sources]
- https://doi.org/10.1364/AO.20.003027
- https://doi.org/10.1117/12.309600
- https://www.osti.gov/servlets/purl/310916
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 12
EUV REFLECTIVE OPTICS
12 / 20
HISTORICAL CONTEXT
EUV mirror는 수십 년의 thin-film·interface·optical theory가 만든 기술이다
1972
DESIGN PRINCIPLE
Spiller
Low-loss reflection coatings
1980
CONTROLLED FABRICATION
Spiller et al.
soft-X-ray mirrors
1981
THEORY FORMALIZED
Underwood & Barbee
Bragg diffractors
1998
EUVL PERFORMANCE
Montcalm et al.
≈67.5% @ 13.4 nm
2001
INTERFACE ENGINEERING
Bajt et al.
≈70% @ 13.5 nm
어느 날 갑자기 등장한 거울이 아니라, weak interface reflection을 제조 가능한 multilayer mirror로 바꾼 누적 혁신
Reference · Spiller 1972 · 10.1063/1.1654189 | Spiller et al. 1980 · 10.1063/1.91759 | Underwood & Barbee 1981 · 10.1364/AO.20.003027 | Montcalm 1998 · 10.1117/12.309600 | Bajt 2001 · 10.1117/12.450946
Notes: [Sources]
- https://doi.org/10.1063/1.1654189
- https://doi.org/10.1063/1.91759
- https://doi.org/10.1364/AO.20.003027
- https://doi.org/10.1117/12.309600
- https://doi.org/10.1117/12.450946
- https://www.osti.gov/biblio/802924
- 1972는 현대 EUV lithography용 Mo/Si mirror 완성 시점이 아니라 low-loss multilayer-like reflection design principle의 역사적 선행으로 서술함.
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 13
EUV SOURCE
13 / 20
SOURCE FUEL ≠ OPTICAL COATING
Sn은 photon을 만들고, Mo/Si는 만들어진 photon을 반사한다
Sn → highly ionized plasma → 13.5 nm photon → Mo/Si optics → scanner
SN · SOURCE FUEL
PHOTON GENERATION
WHY SN?
Highly ionized plasma가 13.5 nm 근처에 강한 emission을 만들고, Mo/Si reflective band와 정합된다.
HISTORICAL CHOICE
초기 후보에는 Xe · Li · Sn 등이 있었다. HVM source power와 conversion-efficiency development를 거치며 Sn LPP가 주류가 됐다.
MO/SI · OPTICAL COATING
PHOTON TRANSPORT
WHAT MO/SI DOES
이미 생성된 13.5 nm EUV를 각 mirror surface에서 최대한 보존해 다음 optical element로 전달한다.
SN TRADE-OFF
Metal debris · vapor · collector contamination → mass-limited droplet, debris mitigation, collector protection이 source architecture의 핵심이 된다.
Sn 효율을 Xe 대비 ‘5–10×’로 단정하지 않는다: 여기서는 검증된 primary source가 뒷받침하는 정성 비교만 사용한다.
Reference · J. Optics · EUV source material review (2022); JMM · LPP source technology; AIP · Sn debris mitigation
Notes: [Sources]
- https://doi.org/10.1088/2040-8986/ac5a7e
- https://doi.org/10.1117/1.JMM.11.2.021111
- https://doi.org/10.1063/5.0200896
- https://www.imec-int.com/en/articles/high-na-euvl-next-major-step-lithography
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 14
EUV SOURCE
14 / 20
SN LASER-PRODUCED PLASMA
Droplet 하나는 shaping·plasma·emission을 거쳐 EUV pulse가 된다
→
→
→
→
→
→
→
01
Molten Sn
droplet
generation
02
Moving target
fast droplet
03
Pre-pulse
pancake /
expanded target
04
Main pulse
high-power
CO₂ laser
05
Plasma
vaporization +
ionization
06
Emission
13.5 nm
EUV photon
07
Collector
capture EUV
08
Scanner
optical path
Laser energy가 13.5 nm로 직접 변환되는 것이 아니다.
Laser가 Sn을 plasma화하고, highly ionized Sn plasma의 electronic transitions가 EUV photon을 방출한다.
OPERATING SCALE
ULTRAFAST REPETITIVE SOURCE
≈ 25 µm
≈ 70 m/s
50,000× / s
moving target
TIN DROPLET
DROPLET VELOCITY
LASER INTERACTIONS
NOT A CONTINUOUSLY LIT LAMP
Reference · ASML · Light & lasers (25 µm, 70 m/s, 50,000 interactions/s)
Notes: [Sources]
- https://www.asml.com/en/technology/lithography-principles/light-and-lasers
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 15
EUV SOURCE
15 / 20
THROUGHPUT ≠ DOSE ACCURACY
Power는 dose를 빨리 채우고, stability는 dose를 정확히 맞춘다
POWER
Dose를 빨리 채우는 능력
STABILITY
Dose를 정확히 맞추는 능력
AVERAGE SOURCE POWER ↑
EXPOSURE TIME ↓
P₁
P₂
P₃
Same target dose
→ shorter exposure time
PROCESS MARGIN
Throughput을 유지하면서 higher-dose resist/process를 선택할 여지가 생겨 stochastic defect trade-off에 유리할 수 있다.
DOSE CONTROL
PULSE-TO-PULSE + SCANNER SYNC
TARGET
Average power가 같아도 pulse variation · dose control · synchronization이 다르면 dose accuracy는 달라진다.
Higher source power ≠ automatically lower dose error
Roadmap 수치는 official primary source의 시점·맥락과 함께만 사용
Reference · ASML 2025 Annual Report · source-power development context; ASML · Light & lasers
Notes: [Sources]
- https://www.asml.com/en/investors/annual-report/2025/strategy-and-stories
- https://www.asml.com/en/technology/lithography-principles/light-and-lasers
- 1000 W는 2025년 4월 demonstration context이며 commercial HVM source로 단정하지 않음. Triple-pulse architecture는 이 슬라이드에서 사용하지 않음.
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 16
HIGH-NA EUV
16 / 20
NXE = 0.33 NA · EXE = 0.55 NA
High-NA는 13.5 nm를 유지한 채 NA를 0.33에서 0.55로 높인다
LOW-NA EUV · NXE
NA 0.33
HIGH-NA EUV · EXE
NA 0.55
0.33
0.55
≈ 13 nm
≈ 8 nm
PRODUCTION RESOLUTION
PRODUCTION RESOLUTION
EXE는 NXE 대비 single exposure에서 약 1.7× smaller feature를 print할 수 있다.
Reference · ASML · NXE:3400C (NA 0.33, 13 nm); EXE:5200B (NA 0.55, 8 nm, 1.7× smaller feature)
Notes: [Sources]
- https://www.asml.com/en/products/euv-lithography-systems/twinscan-nxe3400c
- https://www.asml.com/products/euv-lithography-systems/twinscan-exe-5200b
- https://www.asml.com/en/company/stories/2024/5-things-high-na-euv
- Single exposure는 critical pattern을 multiple lithography decomposition으로 나누지 않고 한 번의 exposure에서 구현하는 resolution capability라는 의미로 사용함.
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 17
HIGH-NA EUV
17 / 20
MAGNIFICATION COMES FROM MIRROR GEOMETRY
Anamorphic optics는 reticle angle 문제를 4×/8× projection으로 푼다
Mo/Si coating = EUV reflectivity · Projection mirror curvature / position / arrangement = focusing + magnification
NXE · ISOMORPHIC
4× / 4×
RETICLE FIELD
→
WAFER FIELD
X 4×
Y 4×
EXE · ANAMORPHIC
4× / 8×
RETICLE FIELD
→
HALF-SIZE FIELD
X 4×
Y 8×
WHY ANAMORPHIC?
NA 0.55에서 기존 4×/4× geometry를 유지하면 reticle incidence angle이 커져 reflectivity와 imaging에 부담이 생긴다.
TRADE-OFF
한 방향 8× demagnification으로 angle을 관리하는 대신 exposure field가 한 방향으로 절반이 된다.
Reference · ASML · 5 things you should know about High-NA EUV lithography; ZEISS · High-NA EUV lithography
Notes: [Sources]
- https://www.asml.com/en/company/stories/2024/5-things-high-na-euv
- https://www.zeiss.com/semiconductor-manufacturing-technology/inspiring-technology/high-na-euv-lithography.html
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 18
HIGH-NA EUV
18 / 20
OPTICS → FIELD COUNT → MOTION CONTROL
Half-field는 stage dynamics를 새로운 throughput 병목으로 만든다
EXPOSURE FIELD TRADE-OFF
FULL FIELD → HALF FIELD
NXE FULL FIELD
→
EXE HALF FIELD × 2
wafer당 exposure field 수 ↑
같은 throughput을 유지하려면 wafer stage와 reticle stage가 더 빠르게 움직여야 한다.
EXE:5000 STAGE SCALE
ACCELERATION
≈ 8 g
≈ 32 g
WAFER STAGE
RETICLE STAGE
THE HARD PART
수십 g acceleration에서도 imaging · overlay에 필요한 nm-level positioning을 유지해야 한다.
NEW BOTTLENECK
Source power가 exposure-time 병목을 줄이면 stage dynamics · overlay · focus · vibration control이 throughput을 제한할 수 있다.
High-NA의 resolution은 optics가 만들지만, 생산성은 precision mechatronics가 지킨다.
Reference · ASML · 5 things you should know about High-NA EUV lithography (8g wafer stage, 32g reticle stage)
Notes: [Sources]
- https://www.asml.com/en/company/stories/2024/5-things-high-na-euv
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 19
PLATFORM ECONOMICS
19 / 20
SYSTEM VALUE, NOT WAVELENGTH VALUE
EUV는 resolution이 아니라 cost-of-patterning이 이길 때 선택된다
EUV
Platform
Economics
Resolution
single-exposure capability
Patterning complexity
process steps · mask count
Overlay / defect
opportunity reduction
Source
power · stability
PR
sensitivity · stochastic
Scanner
throughput · precision
Cycle time
queue · metrology · rework
Cost
tool + process + yield
DUV + multi-patterning이 더 경제적인 layer라면 EUV가 필수는 아니다.
Reference · Synthesis from ASML platform specifications and imec multi-patterning integration context
Notes: [Sources]
- https://www.asml.com/en/products/euv-lithography-systems
- https://www.asml.com/en/company/stories/2024/5-things-high-na-euv
- https://www.imec-int.com/en/imec-magazine/imec-magazine-march-2017/first-euv-lithography-high-volume-manufacturing-solution-for-n5-beol
- Cost-of-patterning 판단은 source들의 기술·공정 trade-off를 통합한 발표용 synthesis이며 특정 layer에 대한 경제성 수치를 제시하지 않음.
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.

## Slide 20
KEY TAKEAWAYS
20 / 20
REFERENCE MAP
EUV의 가치는 13.5 nm photon을 양산 가능한 pattern으로 바꾸는 데 있다
01
Pattern Transfer
PHOTO의 output은 PR image가 아니라 target film에 남은 pattern이다.
02
Resolution
λ · NA · k₁이 함께 정하며, DUV는 OPC와 multi-patterning으로 한계를 확장했다.
03
EUV Transition
13.5 nm의 흡수 특성이 vacuum · reflective mask · mirror optics를 요구했다.
04
Platform Economics
Source · optics · PR · scanner가 resolution · defect · throughput · cost를 함께 만족해야 한다.
PRIMARY / OFFICIAL REFERENCES
SELECTED
RESOLUTION / K₁ / OPC
ASML · Rayleigh criterion; Pushing k1 further; Computational lithography
DUV
ASML · NXT:2000i / 2050i; Lenses & mirrors; Light & lasers
EUV PLATFORMS
ASML · NXE:3400C; EXE:5200B; 5 things about High-NA EUV
MO/SI MIRRORS
Spiller 1972, 1980; Underwood & Barbee 1981; Montcalm 1998; Bajt 2001
SOURCE / MASK / PATTERNING
SPIE / JMM source papers; imec High-NA EUVL; imec SAQP integration
모든 수치·역사·specification은 각 슬라이드 speaker notes의 [Sources]에서 URL로 추적 가능
Reference · Full URLs are embedded in each slide's [Sources] speaker-note block
Notes: [Sources]
- https://www.asml.com/en/technology/lithography-principles/rayleigh-criterion
- https://www.asml.com/en/technology/lithography-principles/pushing-k1-further
- https://www.asml.com/en/products/computational-lithography
- https://www.asml.com/en/products/duv-lithography-systems/twinscan-nxt2000i
- https://www.asml.com/en/en/products/duv-lithography-systems/twinscan-nxt2050i
- https://www.asml.com/technology/lithography-principles/lenses-and-mirrors
- https://www.asml.com/en/technology/lithography-principles/light-and-lasers
- https://www.asml.com/en/products/euv-lithography-systems/twinscan-nxe3400c
- https://www.asml.com/products/euv-lithography-systems/twinscan-exe-5200b
- https://www.asml.com/en/company/stories/2024/5-things-high-na-euv
- https://doi.org/10.1063/1.1654189
- https://doi.org/10.1063/1.91759
- https://doi.org/10.1364/AO.20.003027
- https://doi.org/10.1117/12.309600
- https://doi.org/10.1117/12.450946
- All visible text and diagrams are native editable PowerPoint objects; no full-slide raster image is used.